Fine-Denier Polyester POY Fibers: Experimental Results and Data

- Date: April 25, 2023

- Location: National Advanced Functional Fiber Innovation Center, Shengze, Jiangsu

- Experimental equipment: POY-FDY melt-spinning test machine LX-POY/FDY-30 (Changzhou Lingxian Textile Machinery Co., Ltd.)
Raw material: PET, intrinsic viscosity 0.67 dL/g

- Experimental objective: To investigate the effects of changes in process conditions on the structure and properties of fine-denier POY fibers

- Experimental plan:

(1) Approximately 10 kg of PET chips will be prepared by Donghua University and dried by the National Innovation Center for Advanced Functional Fibers.

(2) Initially, start the experiments with reference to the planned process conditions in Table 1, and adjust the temperature and pump throughput according to the actual equipment conditions until extrusion is normal; once extrusion is normal, adjust the spinning speed to produce POY; vary winding speed, pump throughput, and spinning temperature separately, winding each sample for 10 min.

Summary Table 1. Melt-Spinning Experimental Data

| Specification: POY; spinneret plate: 0.22/72f; metering pump: 2.4 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Experiment No. | 1# | 2# | 3# | 4# | 5# | 6# |
| Experimental Parameters (Process Parameters) |  |  |  |  |  |  |
| Screw zone 1 (°C) | 285 | 285 | 285 | 285 | 285 | 285 |
| Screw zone 2 (°C) | 285 | 285 | 285 | 285 | 285 | 285 |
| Screw zone 3 (°C) | 298 | 298 | 298 | 298 | 298 | 298 |
| Screw zone 4 (°C) | 298 | 298 | 298 | 298 | 298 | 298 |
| Die temperature (°C) | 298 | 298 | 298 | 298 | 298 | 298 |
| Pump throughput (g/s·hole) | 0.648 | 0.648 | 0.648 | 0.648 | 0.648 | 0.648 |
| Metering pump speed (r/min) | 12 | 12 | 12 | 12 | 12 | 12 |
| Screw pressure (MPa) | 6 | 6 | 6 | 6 | 6 | 6 |
| Spin-pack pressure (MPa) | 6 | 6 | 6 | 6 | 5 | 5 |
| Spin-finish pump speed (r/min) | 30 | 30 | 30 | 30 | 30 | 30 |
| Godet 1 speed (m/min) | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 |
| Godet 3 speed (m/min) | 2750 | 2750 | 2750 | 2750 | 2750 | 2750 |
| Godet 4 speed (m/min) | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 |
| Winding speed (m/min) | 2730 | 2980 | 3230 | 3480 | 3730 | 3980 |
| Property Parameters |  |  |  |  |  |  |
| Single-filament fineness (dtex) | 1.66 | 1.50 | 1.42 | 1.31 | 1.21 | 1.15 |
| Single-filament diameter (mm) | 0.0134 | 0.0129 | 0.0086 | 0.0122 | 0.0105 | 0.0107 |
| Degree of orientation | 0.231 | 0.300 | 0.365 | 0.467 | 0.516 | 0.584 |
| Degree of crystallinity (%) | 3.09 | 9.06 | 6.06 | 4.18 | 4.74 | 5.14 |

Summary Table 2. Melt-Spinning Experimental Data

| Specification: POY; spinneret plate: 0.22/72f; metering pump: 2.4 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Experiment No. | 7# | 8# | 9# | 10# | 11# | 12# |
| Experimental Parameters (Process Parameters) |  |  |  |  |  |  |
| Screw zone 1 (°C) | 285 | 285 | 285 | 285 | 280 | 275 |
| Screw zone 2 (°C) | 285 | 285 | 285 | 290 | 285 | 280 |
| Screw zone 3 (°C) | 298 | 298 | 298 | 293 | 288 | 283 |
| Screw zone 4 (°C) | 298 | 298 | 298 | 293 | 288 | 283 |
| Die temperature (°C) | 298 | 298 | 298 | 293 | 288 | 283 |
| Pump throughput (g/s·hole) | 0.583 | 0.541 | 0.486 | 0.541 | 0.541 | 0.541 |
| Metering pump speed (r/min) | 11 | 10 | 9 | 10 | 10 | 10 |
| Screw pressure (MPa) | 6 | 6 | 6 | 6 | 6 | 6 |
| Spin-pack pressure (MPa) | 4.5 | 4.1 | 3.8 | 4.3 | 4.5 | 4.7 |
| Spin-finish pump speed (r/min) | 30 | 30 | 30 | 30 | 30 | 30 |
| Godet 1 speed (m/min) | 3500 | 3500 | 3500 | 3500 | 3500 | 3500 |
| Godet 3 speed (m/min) | 3500 | 3500 | 3500 | 3500 | 3500 | 3500 |
| Godet 4 speed (m/min) | 3500 | 3500 | 3500 | 3500 | 3500 | 3500 |
| Winding speed (m/min) | 3480 | 3480 | 3480 | 3480 | 3480 | 3480 |
| Property Parameters |  |  |  |  |  |  |
| Single-filament fineness (dtex) | 1.18 | 1.08 | 0.95 | 1.08 | 1.08 | 1.08 |
| Single-filament diameter (mm) | 0.0108 | 0.0104 | 0.0086 | 0.0105 | 0.0114 | 0.0104 |
| Degree of orientation | 0.451 | 0.438 | 0.455 | 0.458 | 0.442 | 0.449 |
| Degree of crystallinity (%) | 3.48 | 9.70 | 9.448 | 4.44 | 6.15 | 6.50 |

Subtable 1. Changing the Spinning Speed

Experiment (1): Vary the spinning speed from 2750 to 4000 m/min; Nos. 1#–6#.

| Specification: POY; spinneret plate: 0.22/72f; metering pump: 2.4 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| No. | 1# | 2# | 3# | 4# | 5# | 6# |
| Screw zone 1 (°C) | 285 | 285 | 285 | 285 | 285 | 285 |
| Screw zone 2 (°C) | 285 | 285 | 285 | 285 | 285 | 285 |
| Screw zone 3 (°C) | 298 | 298 | 298 | 298 | 298 | 298 |
| Screw zone 4 (°C) | 298 | 298 | 298 | 298 | 298 | 298 |
| Die temperature (°C) | 298 | 298 | 298 | 298 | 298 | 298 |
| Metering pump speed (r/min) | 12 | 12 | 12 | 12 | 12 | 12 |
| Screw pressure (MPa) | 6 | 6 | 6 | 6 | 6 | 6 |
| Spin-pack pressure (MPa) | 6 | 6 | 6 | 6 | 5 | 5 |
| Spin-finish pump speed (r/min) | 30 | 30 | 30 | 30 | 30 | 30 |
| Godet 1 speed (m/min) | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 |
| Godet 3 speed (m/min) | 2750 | 2750 | 2750 | 2750 | 2750 | 2750 |
| Godet 4 speed (m/min) | 2750 | 3000 | 3250 | 3500 | 3750 | 4000 |
| Winding speed (m/min) | 2730 | 2980 | 3230 | 3480 | 3730 | 3980 |
| Fineness (dtex) | 1.66 | 1.50 | 1.42 | 1.31 | 1.21 | 1.15 |
| Fiber diameter (mm) | 0.0134 | 0.0129 | 0.0086 | 0.0122 | 0.0105 | 0.0107 |
| Degree of orientation | 0.231 | 0.300 | 0.365 | 0.467 | 0.516 | 0.584 |
| Degree of crystallinity (%) | 3.09 | 9.06 | 6.06 | 4.18 | 4.74 | 5.14 |

Subtable 2. Changing the Metering Pump Speed

Experiment (2): Vary the metering pump speed from 9 to 12 r/min; Nos. 4#, 7#–9#.

| Specification: POY; spinneret plate: 0.22/72f; metering pump: 2.4 |  |  |  |  |
| --- | --- | --- | --- | --- |
| No. | 4# | 7# | 8# | 9# |
| Screw zone 1 (°C) | 285 | 285 | 285 | 285 |
| Screw zone 2 (°C) | 285 | 285 | 285 | 285 |
| Screw zone 3 (°C) | 298 | 298 | 298 | 298 |
| Screw zone 4 (°C) | 298 | 298 | 298 | 298 |
| Die temperature (°C) | 298 | 298 | 298 | 298 |
| Metering pump speed (r/min) | 12 | 11 | 10 | 9 |
| Screw pressure (MPa) | 6 | 6 | 6 | 6 |
| Spin-pack pressure (MPa) | 6 | 4.5 | 4.1 | 3.8 |
| Spin-finish pump speed (r/min) | 30 | 30 | 30 | 30 |
| Godet 1 speed (m/min) | 3500 | 3500 | 3500 | 3500 |
| Godet 3 speed (m/min) | 2750 | 3500 | 3500 | 3500 |
| Godet 4 speed (m/min) | 3500 | 3500 | 3500 | 3500 |
| Winding speed (m/min) | 3480 | 3480 | 3480 | 3480 |
| Fineness (dtex) | 1.31 | 1.18 | 1.08 | 0.95 |
| Fiber diameter (mm) | 0.0122 | 0.0108 | 0.0104 | 0.0086 |
| Degree of orientation | 0.467 | 0.451 | 0.438 | 0.455 |
| Degree of crystallinity (%) | 4.18 | 3.48 | 9.70 | 9.448 |

Subtable 3. Changing the Spinning Temperature

Experiment (3): Vary the spinning temperature from 283 to 298 °C; Nos. 8#, 10#–12#.

| Specification: POY; spinneret plate: 0.22/72f; metering pump: 2.4 |  |  |  |  |
| --- | --- | --- | --- | --- |
| No. | 8# | 10# | 11# | 12# |
| Screw zone 1 (°C) | 285 | 285 | 280 | 275 |
| Screw zone 2 (°C) | 285 | 290 | 285 | 280 |
| Screw zone 3 (°C) | 298 | 293 | 288 | 283 |
| Screw zone 4 (°C) | 298 | 293 | 288 | 283 |
| Die temperature (°C) | 298 | 293 | 288 | 283 |
| Metering pump speed (r/min) | 10 | 10 | 10 | 10 |
| Screw pressure (MPa) | 6 | 6 | 6 | 6 |
| Spin-pack pressure (MPa) | 4.1 | 4.3 | 4.5 | 4.7 |
| Spin-finish pump speed (r/min) | 30 | 30 | 30 | 30 |
| Godet 1 speed (m/min) | 3500 | 3500 | 3500 | 3500 |
| Godet 3 speed (m/min) | 3500 | 3500 | 3500 | 3500 |
| Godet 4 speed (m/min) | 3500 | 3500 | 3500 | 3500 |
| Winding speed (m/min) | 3480 | 3480 | 3480 | 3480 |
| Fineness (dtex) | 1.08 | 1.08 | 1.08 | 1.08 |
| Fiber diameter (mm) | 0.0104 | 0.0105 | 0.0114 | 0.0104 |
| Degree of orientation | 0.438 | 0.458 | 0.442 | 0.449 |
| Degree of crystallinity (%) | 9.70 | 4.44 | 6.15 | 6.50 |